## Slide 1
Santiago D. Barrionuevo
Horizon 2020:
Marie Curie Research and Innovation Staff Exchange

## Slide 2
Visiting dates: September 2022 (Ph.D. student) & September 2024 (Postdoc)
Activities:
Conducted synthesis and characterization of two-dimensional (2D) materials aimed at nanoelectronics applications.
Developed several synthesis and transfer techniques specifically tailored for graphene and graphene-derived nanomaterials.
Worked on the advanced characterization of these nanomaterials using high-resolution transmission electron microscopy (HRTEM), scanning transmission electron microscopy (STEM), energy-dispersive X-ray spectroscopy (EDS), and electron energy-loss spectroscopy (EELS).
Santiago D. Barrionuevo
Horizon 2020:
Marie Curie Research and Innovation Staff Exchange

## Slide 3
Twisted Bilayer
Graphene
Graphene
Quantum Dots
Graphene-Metal
Nanohybrids

## Slide 5
Sinthesis and Characterization of CVD Graphene as starting point to obtain Twisted Bilayer Graphene

## Slide 6
Sinthesis and Characterization of Twisted Bilayer Graphene using HRTEM & EELS
Notes: Filtered HRTEM image (left) and simulation (right) of rotated graphene. Moiré patterns are observed for angles of 2.7° (A), 8° (B), and 22° (C). The scale bar corresponds to 5 nm.

## Slide 7
Sinthesis and Characterization of Twisted Bilayer Graphene using HRTEM & EELS
Notes: Filtered HRTEM image (left) and simulation (right) of rotated graphene. Moiré patterns are observed for angles of 2.7° (A), 8° (B), and 22° (C). The scale bar corresponds to 5 nm.

## Slide 8
Notes: Filtered HRTEM image (left) and simulation (right) of rotated graphene. Moiré patterns are observed for angles of 2.7° (A), 8° (B), and 22° (C). The scale bar corresponds to 5 nm.

## Slide 10
Notes: (A) High-resolution transmission electron microscopy (HRTEM) image showing a population of graphene quantum dots (GQDs). (B) To the right, a magnified HRTEM image of an individual GQD is provided. (C) Histogram describing the size distribution for dots larger than 5 nm. Scale bars in figures A and B correspond to 10 and 2 nm, respectively.

## Slide 11
Stacking ABC...ABC
Notes: HRTEM images (top) and FFT patterns (bottom) of few-layer GQDs (A, B, C). Top-view representation of HCP and FCC stacking, respectively (C, F). Yellow, blue, and green spheres represent atoms in layer types A, B, and C, respectively. The scale bar corresponds to 5 nm.

## Slide 12
Twisted Bilayer
Graphene
Graphene
Quantum Dots
Graphene-Metal
Nanohybrids

## Slide 15
Barrionuevo, S. D.; Fioravanti, F.; Nuñez, J. M.; Muñeton Arboleda, D.; Lacconi, G. I.; Bellino, M. G.; Aguirre, M. H.; Ibañez, F. J. Stacking-Configuration-Preserved Graphene Quantum Dots Electrochemically Obtained from CVD Graphene. J. Phys. Chem. C 2024, 128 (3), 1393–1403. https://doi.org/10.1021/acs.jpcc.3c06871.
Llaver, M.; Barrionuevo, S. D.; Troiani, H.; Wuilloud, R. G.; Ibañez, F. J. Highly Selective and Sensitive Fluorescent Determination of Fe3+ within Alcoholic Beverages with 1,5-Diphenylcarbazone-Functionalized Graphene Quantum Dots. Talanta Open 2023, 7, 100202. https://doi.org/10.1016/j.talo.2023.100202.
Barrionuevo, S. D.; Fioravanti, F.; Nuñez, J. M.; Llaver, M.; Aguirre, M. H.; Bellino, M. G.; Lacconi, G. I.; Ibañez, F. J. Efficient Generation of Highly Crystalline Carbon Quantum Dots via Electrooxidation of Ethanol for Rapid Photodegradation of Organic Dyes. J. Mater. Chem. C 2023, 11 (34), 11719–11729. https://doi.org/10.1039/D3TC01774E.
Llaver, M.; Barrionuevo, S. D.; Nuñez, J. M. M.; Chapana, A.; Wuilloud, R. G.; Aguirre, M. H.; Ibañez, F. J. Fluorescent Graphene Quantum Dots-Enhanced Machine Learning for Accurate Detection and Quantification of Hg2+ and Fe3+ in Real Water Samples. Environ. Sci.: Nano 2024. https://doi.org/10.1039/D3EN00702B.
Barrionuevo, S. D.*; Ventre, J*.; Nuñez, J. M.; Renna, A.; Aguirre, M. H.; Bellino, M. G.; Ibañez, F. J. GQDs toward the Spontaneous Synthesis of core-shell Au-graphene Nanohybrid for Non-enzymatic Glucose Detection. ACS Applied Nanomaterials 2025 (Submitted) * Both First Authors
Published Work
Published Thesis
GEFES 2025- Poster Presentation (Spain)
CAFQI 2024- Poster Presentation (Argentina)
ENN 2023 – Poster Presentation (Argentina)
Congress Presentation

## Slide 16
Current Work
Developing an AI assisted Neuromorphic Material Simulator
Summary:
The Neuromorphic Calculator 2025 is a robust simulation platform that streamlines the process of performing first-principles materials calculations with Quantum ESPRESSO.
It has three modes of operation Standard, AI Assisted and Expert level tailored to different user needs.
In the Standard Workflow mode, if you already have a Materials Project ID, you can quickly simulate that material’s properties. In the Assistance mode, if you don’t have a specific ID, AI helps find suitable materials based on your initial data and automatically sets up the simulations. The Expert Workflow mode is for new or unpublished materials, allowing you to customize parameters and refine them over multiple runs. Across all three modes, AI is fully integrated, optimizing simulation parameters, providing literature-backed suggestions, and pulling the latest references with full ACS Nano citations and DOIs.
Notes: The program serves as an integrated simulation platform that automates and streamlines first-principles materials calculations using Quantum ESPRESSO. It guides users through multiple workflows—whether they have a known Materials Project ID or are exploring new, unpublished materials—by generating tailored input files, running comprehensive electronic structure simulations (including SCF, NSCF, band structure, DOS, and EELS calculations), and finally providing AI-driven analysis of the outputs. This comprehensive approach not only reduces manual intervention and error but also offers expert parameter optimization and literature-backed recommendations. Such capabilities are critical for the MELON project, as they enable researchers to efficiently simulate and evaluate the electronic and spintronic properties of advanced materials, thereby accelerating the discovery and design of novel components essential for neuromorphic computing applications.

## Slide 17
Current Work
Developing an AI assisted Neuromorphic Material Simulator
Summary:
The Neuromorphic Calculator 2025 is a robust simulation platform that streamlines the process of performing first-principles materials calculations with Quantum ESPRESSO.
It has three modes of operation tailored to different user needs.
In the Standard Mode mode, if you already have a Materials Project ID, you can quickly simulate that material’s properties.
In the AI Assistance Mode, if you don’t have a specific ID, the AI will help you find suitable materials based on your initial data and requirements, then it will set up the simulations for run it for you.
And in the AI Expert Mode it will help you think about new or unpublished materials, allowing you to customize parameters and refine them over multiple runs. It will ask you to be more involved in the design of each simulation and its going to address , correct and tailor the calculation in order to be consistent with the current literature of the topic you choose e.g.: Neuromorphic, Topological or superconductor materials. The limit is on you!
Across all three modes, AI is fully integrated, generating input files, optimizing simulation parameters, providing literature-backed suggestions, and pulling the latest references with full ACS Nano citations and DOIs. All of this is accomplished using top tier AI models from perplexity AI and also suing the Materials Project Database. In order to provide new tools for AI driven Research
Notes: The program serves as an integrated simulation platform that automates and streamlines first-principles materials calculations using Quantum ESPRESSO. It guides users through multiple workflows—whether they have a known Materials Project ID or are exploring new, unpublished materials—by generating tailored input files, running comprehensive electronic structure simulations (including SCF, NSCF, band structure, DOS, and EELS calculations), and finally providing AI-driven analysis of the outputs. This comprehensive approach not only reduces manual intervention and error but also offers expert parameter optimization and literature-backed recommendations. Such capabilities are critical for the MELON project, as they enable researchers to efficiently simulate and evaluate the electronic and spintronic properties of advanced materials, thereby accelerating the discovery and design of novel components essential for neuromorphic computing applications.

## Slide 18
Current Work
Developing an AI assisted Neuromorphic Material Simulator
DIAGRAMA DE FLUJO DE COMO FUNCIONA SENCILLO
Notes: The program serves as an integrated simulation platform that automates and streamlines first-principles materials calculations using Quantum ESPRESSO. It guides users through multiple workflows—whether they have a known Materials Project ID or are exploring new, unpublished materials—by generating tailored input files, running comprehensive electronic structure simulations (including SCF, NSCF, band structure, DOS, and EELS calculations), and finally providing AI-driven analysis of the outputs. This comprehensive approach not only reduces manual intervention and error but also offers expert parameter optimization and literature-backed recommendations. Such capabilities are critical for the MELON project, as they enable researchers to efficiently simulate and evaluate the electronic and spintronic properties of advanced materials, thereby accelerating the discovery and design of novel components essential for neuromorphic computing applications.

## Slide 19
Current Work
Developing an AI assisted Neuromorphic Material Simulator
Ejemplo de Simulación Bandas y EELS… Si and SrTiO3
Notes: The program serves as an integrated simulation platform that automates and streamlines first-principles materials calculations using Quantum ESPRESSO. It guides users through multiple workflows—whether they have a known Materials Project ID or are exploring new, unpublished materials—by generating tailored input files, running comprehensive electronic structure simulations (including SCF, NSCF, band structure, DOS, and EELS calculations), and finally providing AI-driven analysis of the outputs. This comprehensive approach not only reduces manual intervention and error but also offers expert parameter optimization and literature-backed recommendations. Such capabilities are critical for the MELON project, as they enable researchers to efficiently simulate and evaluate the electronic and spintronic properties of advanced materials, thereby accelerating the discovery and design of novel components essential for neuromorphic computing applications.